## Slide 1
The Higgs Mode:
Ubiquitous in Superconducting Devices
High energy Accelerator Research Organization (KEK)
Innovation Center for Applied Superconducting Accelerators (iCASA)
Takayuki Kubo
This talk is based on the following 3 papers
T. Kubo, Phys. Rev. Applied 22, 044042 (2024) DOI: https://doi.org/10.1103/PhysRevApplied.22.044042
T. Kubo, Phys. Rev. Applied 23, 054091 (2025) DOI: https://doi.org/10.1103/PhysRevApplied.23.054091
T. Kubo, arXiv:2509.09766 (Published soon in a journal) DOI: https://doi.org/10.48550/arXiv.2509.09766
25+5

## Slide 2
Higgs?
Particle physics

## Slide 3
Higgs?
Particle physics
Superconductivity
Oscillation of
superfluid density

## Slide 4
Higgs?
Superconductivity
Oscillation of
superfluid density
The Higgs mode in superconductivity is an effect. It does not appear in standard linear-response theories such as Mattis–Bardeen theory, but it does emerge in nonlinear response:
Nonlinear correction to the current density

## Slide 5
Higgs?
Superconductivity
Oscillation of
superfluid density
The Higgs mode in superconductivity is an effect. It does not appear in standard linear-response theories such as Mattis–Bardeen theory, but it does emerge in nonlinear response:
↓
First harmonic
↓
Third harmonic
Nonlinear correction to the current density

## Slide 6
Higgs?
T. Kubo, arXiv:2509.09766 (Published soon in a journal) DOI: https://doi.org/10.48550/arXiv.2509.09766
Higgs
resonance
↓
First harmonic
↓
Third harmonic
As for the 3rd harmonic response, see also, M. Silaev, Phys. Rev. B 99, 224511 (2019);
P. Derendorf et al., Phys. Rev. B 109, 024510 (2024)

## Slide 7
Higgs?
T. Kubo, arXiv:2509.09766 (Published soon in a journal) DOI: https://doi.org/10.48550/arXiv.2509.09766
Higgs
resonance
Higgs
resonance
↓
First harmonic
↓
Third harmonic
As for the 3rd harmonic response, see also, M. Silaev, Phys. Rev. B 99, 224511 (2019);
P. Derendorf et al., Phys. Rev. B 109, 024510 (2024)

## Slide 8
Higgs?
T. Kubo, arXiv:2509.09766 (Published soon in a journal) DOI: https://doi.org/10.48550/arXiv.2509.09766
GHz (Nb)
GHz (Al)
GHz (Ti)
higher than typical frequencies
of SC devices
Higgs
resonance
Higgs
resonance
Accessible?
As for the 3rd harmonic response, see also, M. Silaev, Phys. Rev. B 99, 224511 (2019);
P. Derendorf et al., Phys. Rev. B 109, 024510 (2024)

## Slide 9
Higgs?
Another way of exciting Higgs mode: dc + ac
A. Moor et al., Phys. Rev. Lett. 118, 047001 (2017)
T. Jujo, J. Phys. Soc. Jpn. 91, 074711 (2022)
T. Kubo, Phys. Rev. Applied 22, 044042 (2024)
T. Kubo, Phys. Rev. Applied 23, 054091 (2025)

## Slide 10
Higgs?
Another way of exciting Higgs mode: dc + ac
A. Moor et al., Phys. Rev. Lett. 118, 047001 (2017)
T. Jujo, J. Phys. Soc. Jpn. 91, 074711 (2022)
T. Kubo, Phys. Rev. Applied 22, 044042 (2024)
T. Kubo, Phys. Rev. Applied 23, 054091 (2025)

## Slide 11
Higgs?
Another way of exciting Higgs mode: dc + ac
↓
Linear
response
↓
Nonlinear
response
A. Moor et al., Phys. Rev. Lett. 118, 047001 (2017)
T. Jujo, J. Phys. Soc. Jpn. 91, 074711 (2022)
T. Kubo, Phys. Rev. Applied 22, 044042 (2024)
T. Kubo, Phys. Rev. Applied 23, 054091 (2025)

## Slide 12
Higgs?
Another way of exciting Higgs mode: dc + ac
↓
Linear
response
↓
Nonlinear
response
A. Moor et al., Phys. Rev. Lett. 118, 047001 (2017)
T. Jujo, J. Phys. Soc. Jpn. 91, 074711 (2022)
T. Kubo, Phys. Rev. Applied 22, 044042 (2024)
T. Kubo, Phys. Rev. Applied 23, 054091 (2025)
GHz (Nb)
GHz (Al)
GHz (Ti)
T. Kubo,
Phys. Rev. Applied 23, 054091 (2025)

## Slide 13
These are the hallmarks of the Higgs mode, which appear at frequencies around , far higher than those of typical superconducting devices.

## Slide 14
These are the hallmarks of the Higgs mode, which appear at frequencies around , far higher than those of typical superconducting devices.
However, its low-frequency tail still plays an important and nontrivial role in superconducting devices.

## Slide 15
These are the hallmarks of the Higgs mode, which appear at frequencies around , far higher than those of typical superconducting devices.
However, its low-frequency tail still plays an important and nontrivial role in superconducting devices.
Some effects of the Higgs mode have, in fact, already manifested themselves, although they have not been recognized as such. A representative example is the current-dependent kinetic inductance.

## Slide 16
(1)
Only weak ac
Outline

## Slide 17
(1)
(2)
Only weak ac
Outline
Only dc current

## Slide 18
(1)
(2)
(3)
Only weak ac
ac + dc
Outline
Semi-phenomenological
approach
Only dc current
S. M. Anlage et al., IEEE Trans. Magn. 25, 1388 (1989).
J. R. Clem and V. G. Kogan, Phys. Rev. B 86, 174521 (2012).
T. Kubo, Phys. Rev. Research 2, 033203 (2020).

## Slide 19
(1)
(2)
(3)
(4)
Only weak ac
ac + dc
ac + dc
Outline
Semi-phenomenological
approach
Microscopic nonequilibrium superconductivity
T. Kubo, Phys. Rev. Applied 22, 044042 (2024)
T. Kubo, Phys. Rev. Applied 23, 054091 (2025)
Only dc current
S. M. Anlage et al., IEEE Trans. Magn. 25, 1388 (1989).
J. R. Clem and V. G. Kogan, Phys. Rev. B 86, 174521 (2012).
T. Kubo, Phys. Rev. Research 2, 033203 (2020).

## Slide 20
(1)
(2)
(3)
(4)
Only weak ac
ac + dc
ac + dc
Outline
Semi-phenomenological
approach
Microscopic nonequilibrium superconductivity
T. Kubo, Phys. Rev. Applied 22, 044042 (2024)
T. Kubo, Phys. Rev. Applied 23, 054091 (2025)
Only dc current
S. M. Anlage et al., IEEE Trans. Magn. 25, 1388 (1989).
J. R. Clem and V. G. Kogan, Phys. Rev. B 86, 174521 (2012).
T. Kubo, Phys. Rev. Research 2, 033203 (2020).

## Slide 21
Kinetic inductance under
an AC perturbation (no DC current)
weak
ac
The kinetic inductivity is defined by

## Slide 22
Kinetic inductance under
an AC perturbation (no DC current)
weak
ac
The kinetic inductivity is defined by
or

## Slide 23
Kinetic inductance under
an AC perturbation (no DC current)
weak
ac
The kinetic inductivity is defined by
or
London eq.

## Slide 24
Kinetic inductance under
an AC perturbation (no DC current)
weak
ac
The kinetic inductivity is defined by
or
London eq.
This basic result already implies that
an oscillation of the superfluid density (i.e., the Higgs mode)
can influence the kinetic inductance.
Very well-known result

## Slide 25
(1)
(2)
(3)
(4)
Only weak ac
Only dc current
ac + dc
ac + dc
Outline
Semi-phenomenological
approach
Microscopic nonequilibrium superconductivity
T. Kubo, Phys. Rev. Applied 22, 044042 (2024)
T. Kubo, Phys. Rev. Applied 23, 054091 (2025)
S. M. Anlage et al., IEEE Trans. Magn. 25, 1388 (1989).
J. R. Clem and V. G. Kogan, Phys. Rev. B 86, 174521 (2012).
T. Kubo, Phys. Rev. Research 2, 033203 (2020).

## Slide 26
Next, we consider only a dc current.
This case is also well understood from decades ago.
See, e.g.,
T. Kubo, Phys. Rev. Research 2, 033203 (2020)
(superfluid momentum)
BCS theory
In the dirty limit

## Slide 27
Next, we consider only a dc current.
This case is also well understood from decades ago.
See, e.g.,
T. Kubo, Phys. Rev. Research 2, 033203 (2020)
(superfluid density)
(superfluid momentum)
BCS theory
In the dirty limit

## Slide 28
Next, we consider only a dc current.
This case is also well understood from decades ago.
See, e.g.,
T. Kubo, Phys. Rev. Research 2, 033203 (2020)
(superfluid density)
(current density)
the maximum value ● is called the depairing current
(superfluid momentum)
BCS theory
In the dirty limit

## Slide 29
Next, we consider only a dc current.
This case is also well understood from decades ago.
See also, T. Kubo, Phys. Rev. Research 2, 033203 (2020); F. Pei-Jen Lin and A. Gurevich, Phys. Rev. B 85, 054513 (2012)
T. Kubo, Phys. Rev. Applied 22, 044042 (2024) DOI: https://doi.org/10.1103/PhysRevApplied.22.044042
(pair potential)
(superfluid momentum)
(current density)
the maximum value ● is called the depairing current

## Slide 30
See also, T. Kubo, Phys. Rev. Research 2, 033203 (2020); F. Pei-Jen Lin and A. Gurevich, Phys. Rev. B 85, 054513 (2012)
T. Kubo, Phys. Rev. Applied 22, 044042 (2024) DOI: https://doi.org/10.1103/PhysRevApplied.22.044042
Density
of
States
Next, we consider only a dc current.
This case is also well understood from decades ago.

## Slide 31
See also, T. Kubo, Phys. Rev. Research 2, 033203 (2020); F. Pei-Jen Lin and A. Gurevich, Phys. Rev. B 85, 054513 (2012)
T. Kubo, Phys. Rev. Applied 22, 044042 (2024) DOI: https://doi.org/10.1103/PhysRevApplied.22.044042
Density
of
States
Density
of
States
Next, we consider only a dc current.
This case is also well understood from decades ago.

## Slide 32
(1)
(2)
(3)
(4)
Only weak ac
Only dc
ac + dc
ac + dc
Outline
Semi-phenomenological
approach
Microscopic nonequilibrium superconductivity
S. M. Anlage et al., IEEE Trans. Magn. 25, 1388 (1989).
J. R. Clem and V. G. Kogan, Phys. Rev. B 86, 174521 (2012).
T. Kubo, Phys. Rev. Research 2, 033203 (2020).
T. Kubo, Phys. Rev. Applied 22, 044042 (2024)
T. Kubo, Phys. Rev. Applied 23, 054091 (2025)

## Slide 33
Let us go back to the definition of ​.
We soon find that it is more complicated than expected.

## Slide 34
Let us go back to the definition of ​.
We soon find that it is more complicated than expected.
S. M. Anlage et al., IEEE Trans. Magn. 25, 1388 (1989).
J. R. Clem and V. G. Kogan, Phys. Rev. B 86, 174521 (2012).
T. Kubo, Physical Review Research 2, 033203 (2020).

## Slide 35
Let us go back to the definition of ​.
We soon find that it is more complicated than expected.
This part can be calculated from the equilibrium theory: the BCS theory
S. M. Anlage et al., IEEE Trans. Magn. 25, 1388 (1989).
J. R. Clem and V. G. Kogan, Phys. Rev. B 86, 174521 (2012).
T. Kubo, Physical Review Research 2, 033203 (2020).

## Slide 36
Let us go back to the definition of ​.
We soon find that it is more complicated than expected.
This looks very much like a nonequilibrium situation.
This part can be calculated from the equilibrium theory: the BCS theory
Dynamics of superfluid density!
S. M. Anlage et al., IEEE Trans. Magn. 25, 1388 (1989).
J. R. Clem and V. G. Kogan, Phys. Rev. B 86, 174521 (2012).
T. Kubo, Physical Review Research 2, 033203 (2020).

## Slide 37
To circumvent the complexity of the nonequilibrium problem,
previous studies introduced the following simplifying assumptions.
S. M. Anlage et al., IEEE Trans. Magn. 25, 1388 (1989).
J. R. Clem and V. G. Kogan, Phys. Rev. B 86, 174521 (2012).
T. Kubo, Physical Review Research 2, 033203 (2020).
Semi-phenomenological approach

## Slide 38
To circumvent the complexity of the nonequilibrium problem,
previous studies introduced the following simplifying assumptions.
S. M. Anlage et al., IEEE Trans. Magn. 25, 1388 (1989).
J. R. Clem and V. G. Kogan, Phys. Rev. B 86, 174521 (2012).
T. Kubo, Physical Review Research 2, 033203 (2020).
Assumption about
dynamics
Fast experiment (Frozen ):
Semi-phenomenological approach

## Slide 39
To circumvent the complexity of the nonequilibrium problem,
previous studies introduced the following simplifying assumptions.
S. M. Anlage et al., IEEE Trans. Magn. 25, 1388 (1989).
J. R. Clem and V. G. Kogan, Phys. Rev. B 86, 174521 (2012).
T. Kubo, Physical Review Research 2, 033203 (2020).
GL theory
or
BCS theory
Assumption about
dynamics
Fast experiment (Frozen ):
Calculate
Semi-phenomenological approach

## Slide 40
To circumvent the complexity of the nonequilibrium problem,
previous studies introduced the following simplifying assumptions.
S. M. Anlage et al., IEEE Trans. Magn. 25, 1388 (1989).
J. R. Clem and V. G. Kogan, Phys. Rev. B 86, 174521 (2012).
T. Kubo, Physical Review Research 2, 033203 (2020).
Slow experiment (oscillating ）:
GL theory
or
BCS theory
Assumption about
dynamics
Fast experiment (Frozen ):
Semi-phenomenological approach
Calculate
Calculate

## Slide 41
We can calculate ​ for any dc bias current.

## Slide 42
We can calculate ​ for any dc bias current. However, here we focus on the small-bias regime (), where the coefficient C in the following expansion can be determined analytically.

## Slide 43
We can calculate ​ for any dc bias current. However, here we focus on the small-bias regime (), where the coefficient C in the following expansion can be determined analytically.
T. Kubo, Physical Review Research 2, 033203 (2020).
Physical Review Research 6, 039002 (2024) [Erratum].
Fast experiment
(Frozen )
BCS theory in the dirty limit

## Slide 44
We can calculate ​ for any dc bias current. However, here we focus on the small-bias regime (), where the coefficient C in the following expansion can be determined analytically.
44
T. Kubo, Physical Review Research 2, 033203 (2020).
Physical Review Research 6, 039002 (2024) [Erratum].
Fast experiment
(Frozen )
Slow experiment
(Oscillating ）
BCS theory in the dirty limit
BCS theory in the dirty limit

## Slide 45
Superconductivity
Oscillation of
superfluid density
Here, let us recall that
the Higgs mode essentially represents
an oscillation of the superfluid density ​.
Then,
does the decades-old assumption of “frozen” and “oscillating” ​ correspond to calculations that neglect and include the Higgs-mode effect, respectively?
Does the difference between C=0.136 and C=0.409
arise from the Higgs mode?

## Slide 46
Semi-phenomenological
approach
Microscopic nonequilibrium superconductivity
(1)
(2)
(3)
(4)
Only weak ac
Only dc
ac + dc
ac + dc
Outline
J. R. Clem and V. G. Kogan, Phys. Rev. B 86, 174521 (2012).
T. Kubo, Phys. Rev. Research 2, 033203 (2020).
T. Kubo, Phys. Rev. Applied 22, 044042 (2024)
T. Kubo, Phys. Rev. Applied 23, 054091 (2025)

## Slide 47
In this case, we need to use the microscopic theory of nonequilibrium superconductivity.
The Keldysh-Eilenberger theory is a microscopic theory of nonequilibrium superconductivity. It is applicable at any temperature () and for arbitrary mean free path. In this sense, it serves as the “theory of everything for conventional superconductivity”.
The Keldysh–Usadel theory represents the dirty-limit reduction of the Keldysh–Eilenberger theory of nonequilibrium superconductivity, applicable at any T ().
T. Kubo, Phys. Rev. Applied 22, 044042 (2024)
A. Moor et al., Phys. Rev. Lett. 118, 047001 (2017)
T. Jujo, J. Phys. Soc. Jpn. 91, 074711 (2022)
T. Kubo, Phys. Rev. Applied 22, 044042 (2024)
T. Kubo, Phys. Rev. Applied 23, 054091 (2025)
T. Kubo, Phys. Rev. Applied 23, 054091 (2025)

## Slide 48
Keldysh–Usadel Equation: DC Current with AC Perturbation
T. Kubo, Phys. Rev. Applied 23, 054091 (2025)
We solve these equations to obtain the AC-induced nonequilibrium corrections ( and ).
Higgs
↓

## Slide 49
Keldysh–Usadel Equation: DC Current with AC Perturbation
T. Kubo, Phys. Rev. Applied 23, 054091 (2025)
To obtain the ac response,
we substitute the solutions (, ) into
We solve these equations to obtain the AC-induced nonequilibrium corrections ( and ).
Higgs
↓

## Slide 50
Instead of showing the rigorous algebraic calculations, we will look at schematic illustrations that represent the final results.

## Slide 51
Instead of showing the rigorous algebraic calculations, we will look at schematic illustrations that represent the final results.

## Slide 52
and
Instead of showing the rigorous algebraic calculations, we will look at schematic illustrations that represent the final results.

## Slide 53
and
Higgs mediated contribution
AAA cotribution
Instead of showing the rigorous algebraic calculations, we will look at schematic illustrations that represent the final results.

## Slide 54
and
Higgs mediated contribution
AAA cotribution
Instead of showing the rigorous algebraic calculations, we will look at schematic illustrations that represent the final results.
Nonequilibrium corrections due to the Doppler fluctuation of flow

## Slide 55
Then, the complex conductivity is given by
and
Higgs mediated contribution
AAA cotribution
Instead of showing the rigorous algebraic calculations, we will look at schematic illustrations that represent the final results.

## Slide 56
Complex conductivity formula
case
Nonequilibrium corrections due to the Doppler fluctuation of flow
Higgs
mediated contribution
AAA
contribution
T. Kubo, Phys. Rev. Applied 23, 054091 (2025)

## Slide 57
Complex conductivity formula
case
case
Nonequilibrium corrections due to the Doppler fluctuation of flow
No Doppler fluctuation
Higgs
mediated contribution
AAA
contribution
T. Kubo, Phys. Rev. Applied 23, 054091 (2025)

## Slide 58
ac dc
T. Kubo,
Phys. Rev. Applied 23, 054091 (2025)

## Slide 59
ac dc
ac dc
Resonance peak due to the Higgs mode.
Already observed in experiments!
S. Nakamura et al.,
PRL 122, 257001 (2019)
T. Kubo,
Phys. Rev. Applied 23, 054091 (2025)
T. Kubo,
Phys. Rev. Applied 23, 054091 (2025)

## Slide 60
For , we can analytically calculate the coefficient C
To calculate the kinetic inductance, we just go back to its definition.

## Slide 61
For , we can analytically calculate the coefficient C
To calculate the kinetic inductance, we just go back to its definition.
case

## Slide 62
case
Higgs
AAA
(23%)
(43%)
For , we can analytically calculate the coefficient C
To calculate the kinetic inductance, we just go back to its definition.
case

## Slide 63
case
Higgs
AAA
(23%)
(43%)
For , we can analytically calculate the coefficient C
T. Kubo, Phys. Rev. Applied 22, 044042 (2024)
T. Kubo, Phys. Rev. Applied 23, 054091 (2025)
To calculate the kinetic inductance, we just go back to its definition.
case
Microscopic theory of
nonequilibrium superconductivity

## Slide 64
case
Higgs
AAA
(23%)
(43%)
For , we can analytically calculate the coefficient C
T. Kubo, Phys. Rev. Applied 22, 044042 (2024)
T. Kubo, Phys. Rev. Applied 23, 054091 (2025)
To calculate the kinetic inductance, we just go back to its definition.
case
Semi-phenomenological
Microscopic theory of
nonequilibrium superconductivity
J. R. Clem and V. G. Kogan, Phys. Rev. B 86, 174521 (2012).
T. Kubo, Physical Review Research 2, 033203 (2020).

## Slide 65
case
Higgs
AAA
(23%)
(43%)
For , we can analytically calculate the coefficient C
T. Kubo, Phys. Rev. Applied 22, 044042 (2024)
T. Kubo, Phys. Rev. Applied 23, 054091 (2025)
To calculate the kinetic inductance, we just go back to its definition.
case
Fast experiment (Frozen )
Semi-phenomenological
Microscopic theory of
nonequilibrium superconductivity
J. R. Clem and V. G. Kogan, Phys. Rev. B 86, 174521 (2012).
T. Kubo, Physical Review Research 2, 033203 (2020).

## Slide 66
case
Higgs
AAA
(23%)
(43%)
For , we can analytically calculate the coefficient C
T. Kubo, Phys. Rev. Applied 22, 044042 (2024)
T. Kubo, Phys. Rev. Applied 23, 054091 (2025)
To calculate the kinetic inductance, we just go back to its definition.
case
Fast experiment (Frozen )
Slow experiment (Oscillating ）
Semi-phenomenological
Microscopic theory of
nonequilibrium superconductivity
J. R. Clem and V. G. Kogan, Phys. Rev. B 86, 174521 (2012).
T. Kubo, Physical Review Research 2, 033203 (2020).

## Slide 67
“C” from the Keldysh-Eilenberger theory, which is a microscopic theory of nonequilibrium superconductivity and is applicable at any temperature () and for arbitrary mean free path.
Consistent with the dirty limit result
obtained from the Keldysh-Usadel

## Slide 68
We have finally come to understand the true meaning of the semi-phenomenological approach: frozen and oscillating
Frozen
The ac frequency is so fast that
the superfluid density cannot follow it.
(Fast experiment)
What has long been believed
[When Does it happen?]

## Slide 69
Frozen
The ac frequency is so fast that
the superfluid density cannot follow it.
(Fast experiment)
Oscillating
The ac frequency is so slow that the superfluid density can follow it.
(Slow experiment)
[When Does it happen?]
What has long been believed
We have finally come to understand the true meaning of the semi-phenomenological approach: frozen and oscillating

## Slide 70
Frozen
The ac frequency is so fast that
the superfluid density cannot follow it.
(Fast experiment)
Oscillating
The ac frequency is so slow that the superfluid density can follow it.
(Slow experiment)
What has long been believed
We have finally come to understand the true meaning of the semi-phenomenological approach: frozen and oscillating
What has been revealed
by the microscopic theory of nonequilibrum superconductivity
[When Does it happen?]
[When Does it happen?]

## Slide 71
Frozen
The ac frequency is so fast that
the superfluid density cannot follow it.
(Fast experiment)
Oscillating
The ac frequency is so slow that the superfluid density can follow it.
(Slow experiment)
What has long been believed
What has been revealed
by the microscopic theory of nonequilibrum superconductivity
(AAA and Higgs contribution)
wrong
We have finally come to understand the true meaning of the semi-phenomenological approach: frozen and oscillating
[When Does it happen?]
[When Does it happen?]

## Slide 72
Summary
case
Higgs
AAA
(23%)
(43%)
case
The Higgs mode is ubiquitous in superconducting devices. The current dependence of the kinetic inductance is a representative example.

## Slide 74
Other works of mine that may interest you:
T. Kubo, On the applicability ranges of Tc formulas for proximity-coupled thin SN and SS bilayers, Japanese Journal of Applied Physics 64, 018001 (2025).
  This is a brief review of Tc formulas of SN and SS bilayers. Because several distinct formulas exist, misuse is common. Please verify that your choice is appropriate. For instance, if a chosen formula yields a Tc that increases with the N-layer thickness, that formula is being applied outside its valid range. The solution is here.
T. Takenaka, T. Kubo et al., Three-Dimensional Niobium Coaxial Cavity with ~0.1 second Lifetime, arXiv:2510.01819.
  In this work, we applied surface-treatment technologies developed for accelerator cavities and achieved a world-record quality factor in this type of quantum-memory cavity for quantum computing applications.
Tc
N thickness
If you encounter this problem,
you’re using the wrong formula!
Me
↓
wrong
correct
←cavity

## Slide 75
Backup ()

## Slide 76
(dirty)
T. Kubo, Phys. Rev. Applied 22, 044042 (2024)
Analogue Rs(E) curve
in ac+dc system
dc: arbitrary strength
ac: perturbation

## Slide 77
(dirty)
T. Kubo, Phys. Rev. Applied 22, 044042 (2024)
Let’s see the orange curves (),which correspond to 7GHz for Nb.
7GHz for Nb

## Slide 78
(dirty)
T. Kubo, Phys. Rev. Applied 22, 044042 (2024)
Let’s see the orange curves (),which correspond to 7GHz for Nb.
Dotted curve:

## Slide 79
(dirty)
T. Kubo, Phys. Rev. Applied 22, 044042 (2024)
Let’s see the orange curves (),which correspond to 7GHz for Nb.
Dotted curve:
Dashed curve:
Re[
Significant contribution from
the direct AAA action term

## Slide 80
(dirty)
T. Kubo, Phys. Rev. Applied 22, 044042 (2024)
Let’s see the orange curves (),which correspond to 7GHz for Nb.
Dotted curve:
Dashed curve:
Re[
Solid curve:
Re[
Significant contribution from
the direct AAA action term

## Slide 81
(dirty)
T. Kubo, Phys. Rev. Applied 22, 044042 (2024)
The analogue anti Q-slope is pronounced as the frequency increases
The key player is the direct AAA photon action
Big clue to understand the pronounced anti Q-slope with increasing frequency
3.6 GHz for Nb
7 GHz for Nb
14 GHz for Nb
36 GHz for Nb
1.8 GHz for Nb