## Slide 1
Nonequilibrium Corrections and Higgs Mode
in Superconducting Devices:
Unraveling the Pronounced Anti-Q Slope in High-Frequency regime
and Current-Dependent Kinetic Inductance
High energy Accelerator Research Organization (KEK)
Takayuki Kubo
This talk is based on the following 3 papers
T. Kubo, Phys. Rev. Applied 22, 044042 (2024) DOI: https://doi.org/10.1103/PhysRevApplied.22.044042
T. Kubo, Phys. Rev. Applied 23, 054091 (2025) DOI: https://doi.org/10.1103/PhysRevApplied.23.054091
T. Kubo, arXiv:2509.09766 DOI: https://doi.org/10.48550/arXiv.2509.09766
Sep.25
THA06

## Slide 2
One of the main theoretical questions in SRF physics is how the curve depends on frequency.
M. Martinello et al., Phys. Rev. Lett. 121, 224801 (2018)
DOI: https://doi.org/10.1103/PhysRevLett.121.224801

## Slide 3
One of the main theoretical questions in SRF physics is how the curve depends on frequency.
P. Dhakal, B. D. Khanal, A. Gurevich, and G. Ciovati, Phys. Rev. Accel. Beams 27, 062001 (2024) DOI: https://doi.org/10.1103/PhysRevAccelBeams.27.062001

## Slide 4
M. Martinello et al., Phys. Rev. Lett. 121, 224801 (2018)
DOI: https://doi.org/10.1103/PhysRevLett.121.224801
P. Dhakal, B. D. Khanal, A. Gurevich, and G. Ciovati,
Phys. Rev. Accel. Beams 27, 062001 (2024) DOI: https://doi.org/10.1103/PhysRevAccelBeams.27.062001
One of the main theoretical questions in SRF physics is how the curve depends on frequency.
There is a threshold around 1 GHz: below it, the curve bends upward; above it, the curve bends downward — the so-called anti-Q slope.
N-dope
T=2K
650 MHz
1.3 GHz
3.9 GHz
2.6 GHz

## Slide 5
To address this problem, we consider
a superconductor carrying a DC current and perturbed by a weak AC field.
This approach provides a key clue to understanding the issue.
The detailed discussions are found here:
T. Kubo, Phys. Rev. Applied 22, 044042 (2024) DOI: https://doi.org/10.1103/PhysRevApplied.22.044042
T. Kubo, Phys. Rev. Applied 23, 054091 (2025) DOI: https://doi.org/10.1103/PhysRevApplied.23.054091

## Slide 6
If the AC field is absent, this reduces to a problem of equilibrium superconductivity.
That case was already well understood decades ago.
See also, T. Kubo, Phys. Rev. Research 2, 033203 (2020); F. Pei-Jen Lin and A. Gurevich, Phys. Rev. B 85, 054513 (2012)
T. Kubo, Phys. Rev. Applied 22, 044042 (2024) DOI: https://doi.org/10.1103/PhysRevApplied.22.044042

## Slide 7
If the AC field is absent, this reduces to a problem of equilibrium superconductivity.
That case was already well understood decades ago.
See also, T. Kubo, Phys. Rev. Research 2, 033203 (2020); F. Pei-Jen Lin and A. Gurevich, Phys. Rev. B 85, 054513 (2012)
T. Kubo, Phys. Rev. Applied 22, 044042 (2024) DOI: https://doi.org/10.1103/PhysRevApplied.22.044042

## Slide 8
If the AC field is absent, this reduces to a problem of equilibrium superconductivity.
That case was already well understood decades ago.
See also, T. Kubo, Phys. Rev. Research 2, 033203 (2020); F. Pei-Jen Lin and A. Gurevich, Phys. Rev. B 85, 054513 (2012)
T. Kubo, Phys. Rev. Applied 22, 044042 (2024) DOI: https://doi.org/10.1103/PhysRevApplied.22.044042

## Slide 9
However, once an AC field is present, the problem becomes much more complicated. In that case, we need to use the theory of nonequilibrium superconductivity.
The Keldysh-Eilenberger theory is a microscopic theory of nonequilibrium superconductivity. It is applicable at any temperature () and for arbitrary mean free path. In this sense, it serves as the “theory of everything for conventional superconductivity”.
The Keldysh–Usadel theory represents the dirty-limit reduction of the Keldysh–Eilenberger theory of nonequilibrium superconductivity, applicable at any T ().
T. Kubo, Phys. Rev. Applied 22, 044042 (2024)
A. Moor et al., Phys. Rev. Lett. 118, 047001 (2017)
T. Jujo, J. Phys. Soc. Jpn. 91, 074711 (2022)
T. Kubo, Phys. Rev. Applied 22, 044042 (2024)
T. Kubo, Phys. Rev. Applied 23, 054091 (2025)
T. Kubo, Phys. Rev. Applied 23, 054091 (2025)

## Slide 10
Keldysh–Usadel Equation: DC Current with AC Perturbation
T. Kubo, Phys. Rev. Applied 23, 054091 (2025)
We solve these equations to obtain the AC-induced nonequilibrium corrections ( and ).
Higgs
↓

## Slide 11
Keldysh–Usadel Equation: DC Current with AC Perturbation
T. Kubo, Phys. Rev. Applied 23, 054091 (2025)
We solve these equations to obtain the AC-induced nonequilibrium corrections ( and ).
Higgs?
Higgs
↓
Particle physics

## Slide 12
Keldysh–Usadel Equation: DC Current with AC Perturbation
T. Kubo, Phys. Rev. Applied 23, 054091 (2025)
We solve these equations to obtain the AC-induced nonequilibrium corrections ( and ).
Higgs?
Particle physics
Superconductivity
Oscillation of
superfluid density
Higgs
↓

## Slide 13
Keldysh–Usadel Equation: DC Current with AC Perturbation
T. Kubo, Phys. Rev. Applied 23, 054091 (2025)
We solve these equations to obtain the AC-induced nonequilibrium corrections ( and ).
Higgs?
The Higgs mode in superconductivity is an effect. It does not appear in standard linear-response theories such as Mattis–Bardeen, but it does emerge in nonlinear response. In our case, we apply both DC and AC fields. As a result, the Higgs mode shows up as , and responds linearly to the AC field.
Higgs
↓
Oscillation of
superfluid density
Superconductivity
See the famous review paper:
R. Shimano and N. Tsuji,
Annu. Rev. Condens. Matter Phys. 11, 103 (2020)

## Slide 14
Keldysh–Usadel Equation: DC Current with AC Perturbation
T. Kubo, Phys. Rev. Applied 23, 054091 (2025)
We solve these equations to obtain the AC-induced nonequilibrium corrections ( and ).
Higgs
↓

## Slide 15
Keldysh–Usadel Equation: DC Current with AC Perturbation
T. Kubo, Phys. Rev. Applied 23, 054091 (2025)
To obtain the ac response,
we substitute the solutions (, ) into
We solve these equations to obtain the AC-induced nonequilibrium corrections ( and ).
Higgs
↓

## Slide 16
Instead of showing the rigorous algebraic calculations, we will look at schematic illustrations that represent the final results.

## Slide 17
Instead of showing the rigorous algebraic calculations, we will look at schematic illustrations that represent the final results.

## Slide 18
and
Instead of showing the rigorous algebraic calculations, we will look at schematic illustrations that represent the final results.

## Slide 19
and
Higgs mediated contribution
AAA cotribution
Instead of showing the rigorous algebraic calculations, we will look at schematic illustrations that represent the final results.

## Slide 20
and
Higgs mediated contribution
AAA cotribution
Instead of showing the rigorous algebraic calculations, we will look at schematic illustrations that represent the final results.
Nonequilibrium corrections due to the Doppler fluctuation of flow

## Slide 21
Then, the complex conductivity is given by
and
Higgs mediated contribution
AAA cotribution
Instead of showing the rigorous algebraic calculations, we will look at schematic illustrations that represent the final results.

## Slide 22
Complex conductivity formula
case
Nonequilibrium corrections due to the Doppler fluctuation of flow
Higgs
mediated contribution
AAA
contribution
T. Kubo, Phys. Rev. Applied 23, 054091 (2025)

## Slide 23
Complex conductivity formula
case
case
Nonequilibrium corrections due to the Doppler fluctuation of flow
No Doppler fluctuation
Higgs
mediated contribution
AAA
contribution
T. Kubo, Phys. Rev. Applied 23, 054091 (2025)

## Slide 24
ac dc
T. Kubo,
Phys. Rev. Applied 23, 054091 (2025)

## Slide 25
ac dc
ac dc
Resonance peak due to the Higgs mode.
Already observed in experiments!
S. Nakamura et al.,
PRL 122, 257001 (2019)
T. Kubo,
Phys. Rev. Applied 23, 054091 (2025)
T. Kubo,
Phys. Rev. Applied 23, 054091 (2025)

## Slide 26
Direct AAA photon action
Higgs mediated contribution
The contributions from the nonequilibrium corrections are significant even at low frequencies
Significantly contributes to
even at low frequencies
Significantly contributes to
,
even at low frequencies

## Slide 27
Direct AAA photon action
Higgs mediated contribution
The contributions from the nonequilibrium corrections are significant even at low frequencies
Surface resistance
or
quality factor
Significantly contributes to
even at low frequencies
Significantly contributes to
,
even at low frequencies

## Slide 28
Direct AAA photon action
Higgs mediated contribution
The contributions from the nonequilibrium corrections are significant even at low frequencies
Surface resistance
or
quality factor
Kinetic inductance
Significantly contributes to
even at low frequencies
Significantly contributes to
,
even at low frequencies

## Slide 29
Biproduct: the theory of current-dependent kinetic inductance is now established.
case
Higgs
AAA
(23%)
(43%)
43% comes from Higgs!
For , we can analytically calculate the coefficient C:
T. Kubo, Phys. Rev. Applied 22, 044042 (2024)
T. Kubo, Phys. Rev. Applied 23, 054091 (2025)

## Slide 30
(dirty)
T. Kubo, Phys. Rev. Applied 22, 044042 (2024)
Analogue Rs(E) curve
in ac+dc system
dc: arbitrary strength
ac: perturbation

## Slide 31
(dirty)
T. Kubo, Phys. Rev. Applied 22, 044042 (2024)
Let’s see the orange curves (),which correspond to 7GHz for Nb.
7GHz for Nb

## Slide 32
(dirty)
T. Kubo, Phys. Rev. Applied 22, 044042 (2024)
Let’s see the orange curves (),which correspond to 7GHz for Nb.
Dotted curve:

## Slide 33
(dirty)
T. Kubo, Phys. Rev. Applied 22, 044042 (2024)
Let’s see the orange curves (),which correspond to 7GHz for Nb.
Dotted curve:
Dashed curve:
Re[
Significant contribution from
the direct AAA action term

## Slide 34
(dirty)
T. Kubo, Phys. Rev. Applied 22, 044042 (2024)
Let’s see the orange curves (),which correspond to 7GHz for Nb.
Dotted curve:
Dashed curve:
Re[
Solid curve:
Re[
Significant contribution from
the direct AAA action term

## Slide 35
(dirty)
T. Kubo, Phys. Rev. Applied 22, 044042 (2024)
The analogue anti Q-slope is pronounced as the frequency increases
The key player is the direct AAA photon action
Big clue to understand the pronounced anti Q-slope with increasing frequency
3.6 GHz for Nb
7 GHz for Nb
14 GHz for Nb
36 GHz for Nb
1.8 GHz for Nb

## Slide 37
Nonequilibrium
Nonlinear Response theory of
amplitude dependent conductivity
under strong ac field
The detailed discussions are found here:
T. Kubo, arXiv:2509.09766 DOI: https://doi.org/10.48550/arXiv.2509.09766

## Slide 38
We do not consider any dc bias.
We consider a superconductor under a strong ac field

## Slide 39
Keldysh–Usadel Equation for SC under a strong ac field
To obtain the current response,
we substitute the solutions (, ) into
We solve these equations to obtain the nonequilibrium corrections ( and ).
← Linear response
← Nonlinear correction of
Much different
from the ac+dc case
arXiv:2509.09766

## Slide 40
Schematically, the results can be illustrated as
Linear
response
Nonlinear corrections
and

## Slide 41
Schematically, the results can be illustrated as
Linear
response
Nonlinear corrections
and
Time dependent :
Higgs
Time averaged :
Eliashberg effect
Note: This theory automatically includes
the Eliashberg effect (microwave-induced gap enhancement) as well as the Higgs-mode contribution.

## Slide 42
Eliashberg effect
Higgs mode
arXiv:2509.09766
arXiv:2509.09766
See also,
M. Silaev, Phys. Rev. B 99, 224511 (2019) P. Derendorf, A. F. Volkov, and I. M. Eremin, Phys. Rev. B 109, 024510 (2024)

## Slide 43
Nonlinear correction
Higgs
Contribution:
Time dependent
Eliashberg
Contribution:
Time averaged
arXiv:2509.09766

## Slide 44
Results

## Slide 45
Results
The resonance peak at Δ
comes from the Higgs mode

## Slide 46
Results
The resonance peak at Δ
comes from the Higgs mode
At lower frequencies,
is a decreasing function of the ac amplitude (q).

## Slide 47
Results
The resonance peak at Δ
comes from the Higgs mode
At lower frequencies,
is a decreasing function of the ac amplitude (q).
The AAA term is
the dominant contributor
at low frequencies

## Slide 48
360MHz for Nb
720MHz for Nb
3.6GHz for Nb
1.8GHz for Nb
ac amplitude dependent dissipative conductivity
Note: this corresponds to a few (mT)
arXiv:2509.09766
Dirty limit ()

## Slide 49
360MHz for Nb
720MHz for Nb
3.6GHz for Nb
1.8GHz for Nb
ac amplitude dependent dissipative conductivity
Note: this corresponds to a few (mT)
arXiv:2509.09766
Dirty limit ()
Experiments:
Moderately dirty ()
M. Martinello et al., Phys. Rev. Lett. 121, 224801 (2018)
DOI: https://doi.org/10.1103/PhysRevLett.121.224801

## Slide 50
ac amplitude dependent dissipative conductivity
Experiments:
Moderately dirty ()
M. Martinello et al., Phys. Rev. Lett. 121, 224801 (2018)
DOI: https://doi.org/10.1103/PhysRevLett.121.224801
To deal with the red-framed region, the theory must be extended nonperturbatively to capture the quasiparticle spectrum modified by strong AC currents.
A. Gurevich, Phys. Rev. Lett. 113, 087001 (2014)
T. Kubo and A. Gurevich, Phys. Rev. B 100, 064522 (2019)
The theory of SRF
T. Kubo, arXiv:2509.09766 (2025)
Nonperturbative extension like the previous studies:

## Slide 51
Summary
The frequency dependent anti-Q slope can be explained by the nonlinear AAA term. The Eliashberg effect and the Higgs mode contributions are not significant in SRF regime.
We are only one step away from establishing the SRF theory. A nonperturbative extension of the present theory will complete it.
AAA term
Eliashberg and Higgs
→ Nonequilibrium Nonlinear Nonperturbative ac response theory

## Slide 52
Oct. 2016
Norfolk
Acknowledgement
This work was conducted independently, and I take full responsibility for its content.
Nevertheless, its foundation stems from my visit to Alex Gurevich at Old Dominion University in 2016 and from my sabbatical there between 2017 and 2019.
I deeply appreciate his warm hospitality and invaluable support during those stays.

## Slide 54
360MHz for Nb
720MHz for Nb
3.6GHz for Nb
1.8GHz for Nb
arXiv:2509.09766
Dirty limit ()
360MHz for Nb
3.6GHz for Nb
36GHz for Nb
7.2GHz for Nb
Effects of the inelastic scattering (e.g., electron-phonon) rate
arXiv:2509.09766
appendix