## Slide 1
International Workshop on Intrinsic Josephson Junctions and Nanostructured Superconducting Physics (Dec. 6, 2025)
Superconducting Resonators: a Crossroads of
High-Energy Accelerators, Astrophysical Detectors,
Condensed Matter Theory, and Quantum Computing
High energy Accelerator Research Organization (KEK)
Innovation Center for Applied Superconducting Accelerators (iCASA)
Takayuki Kubo

## Slide 2
https://linearcollider.org/conditions-for-material-usage/
Here we use the International Linear Collider (ILC), an electron–positron Higgs factory, as an example, but the European X-ray Free-Electron Laser (European XFEL) in Germany and the Linac Coherent Light Source II (LCLS-II) at SLAC in California are also based on similar superconducting RF linac technology.

## Slide 3
https://linearcollider.org/conditions-for-material-usage/

## Slide 4
https://linearcollider.org/conditions-for-material-usage/

## Slide 5
https://linearcollider.org/conditions-for-material-usage/
Cryomodule

## Slide 6
https://linearcollider.org/conditions-for-material-usage/
9-cell Nb Accelerator
Cavity (1.3 GHz)
Cryomodule

## Slide 7
9-cell Nb Accelerator
Cavity (1.3 GHz)
Single-cell Nb accelerator cavity (1.3 GHz)

## Slide 8
Electric field
distribution
Single-cell Nb accelerator cavity (1.3 GHz)

## Slide 9
Electric field
distribution
Magnetic field
distribution
Single-cell Nb accelerator cavity (1.3 GHz)

## Slide 10
Electric field
distribution
Magnetic field
distribution
Single-cell Nb accelerator cavity (1.3 GHz)
There are two key performance metrics
Accelerating electric field
Quality factor (smallness of dissipation)

## Slide 11
There are two key performance metrics
Accelerating electric field
Quality factor (smallness of dissipation)
Electric field
distribution
Magnetic field
distribution
Single-cell Nb accelerator cavity (1.3 GHz)
Nb
T Kubo et al., IPAC2014, Dresden, Germany, WEPRI022, p.2519
https://doi.org/10.18429/JACoW-IPAC2014-WEPRI022

## Slide 12
There are two key performance metrics
Accelerating electric field
Quality factor (smallness of dissipation)
Electric field
distribution
Magnetic field
distribution
At 40MV/m,
microwave B field
reaches
Nb
T Kubo et al., IPAC2014, Dresden, Germany, WEPRI022, p.2519
https://doi.org/10.18429/JACoW-IPAC2014-WEPRI022

## Slide 13
(⌐■_■) good
170mT
0mT
85mT
of Nb
of Nb
210mT
0 MV/m
20 MV/m
40
MV/m
50
MV/m
Nb
T Kubo et al., IPAC2014, Dresden, Germany, WEPRI022, p.2519
https://doi.org/10.18429/JACoW-IPAC2014-WEPRI022
Low field (Meissner state)
Note: Cavities are operated under the Meissner state
Electric field
distribution
Magnetic field
distribution

## Slide 14
170mT
0mT
85mT
of Nb
of Nb
210mT
0 MV/m
20 MV/m
40
MV/m
50
MV/m
(⌐■_■) good
Nb
T Kubo et al., IPAC2014, Dresden, Germany, WEPRI022, p.2519
https://doi.org/10.18429/JACoW-IPAC2014-WEPRI022
Low field (Meissner state)
Note: Cavities are operated under the Meissner state
Electric field
distribution
Magnetic field
distribution

## Slide 15
170mT
0mT
85mT
of Nb
of Nb
210mT
0 MV/m
20 MV/m
40
MV/m
50
MV/m
(⌐■_■) good
Nb
T Kubo et al., IPAC2014, Dresden, Germany, WEPRI022, p.2519
https://doi.org/10.18429/JACoW-IPAC2014-WEPRI022
Low field (Meissner state)
Note: Cavities are operated under the Meissner state
Electric field
distribution
Magnetic field
distribution

## Slide 16
＼(^o^)／ｵﾜﾀ
I’m doomed
170mT
0mT
85mT
of Nb
of Nb
210mT
0 MV/m
20 MV/m
40
MV/m
50
MV/m
Nb
T Kubo et al., IPAC2014, Dresden, Germany, WEPRI022, p.2519
https://doi.org/10.18429/JACoW-IPAC2014-WEPRI022
High field (vortex state)
Note: Cavities are operated under the Meissner state
Electric field
distribution
Magnetic field
distribution

## Slide 17
Note: Cavities are operated under the Meissner state
170mT
0mT
85mT
of Nb
of Nb
210mT
0 MV/m
20 MV/m
40
MV/m
50
MV/m
:​ the lower critical field, above which the Meissner state becomes energetically unfavorable. : the superheating field, which represents the stability limit of the Meissner state. Ultimate limit for the ideal material.
G. Catelani and J. P. Sethna,
Phys. Rev. B 78, 224509 (2008)
F. Pei-Jen Lin and A. Gurevich,
Phys. Rev. B 85, 054513 (2012)
T. Kubo, Phys. Rev. Research 2, 033203 (2020)
T. Kubo, Supercond.Sci. Tecnol. 34, 045006 (2021)
Nb
T Kubo et al., IPAC2014, Dresden, Germany, WEPRI022, p.2519
https://doi.org/10.18429/JACoW-IPAC2014-WEPRI022
Electric field
distribution
Magnetic field
distribution

## Slide 18
There are two key performance metrics
Accelerating electric field
Quality factor (smallness of dissipation)
Electric field
distribution
Magnetic field
distribution
Nb
T Kubo et al., IPAC2014, Dresden, Germany, WEPRI022, p.2519
https://doi.org/10.18429/JACoW-IPAC2014-WEPRI022

## Slide 19
There are two key performance metrics
Accelerating electric field
Quality factor (smallness of dissipation)
Electric field
distribution
Magnetic field
distribution
Nb
: dissipation per RF cycle
: how many cycles it takes for the stored energy to completely dissipate
This is the key parameter common to all superconducting resonators.
T Kubo et al., IPAC2014, Dresden, Germany, WEPRI022, p.2519
https://doi.org/10.18429/JACoW-IPAC2014-WEPRI022

## Slide 20
Overview of
energy dissipation mechanisms in superconducting resonators
What are the causes of dissipation?

## Slide 21
Surface resistance
Higher T
Lower T
1.3GHz Nb cavity
e.g., bulk Nb

## Slide 22
Surface resistance
Higher T
Lower T
1.3GHz Nb cavity
e.g., bulk Nb

## Slide 23
At a higher T (K)
Surface resistance
Higher T
Lower T
The contribution from thermally activated quasiparticles decreases exponentially [].
1.3GHz Nb cavity
e.g., bulk Nb

## Slide 24
Higher T
Lower T
At a lower T (K)
Surface resistance
The quasiparticle contribution is exponentially suppressed (dashed curve), but other mechanisms can dominate at low temperatures.
1.3GHz Nb cavity

## Slide 25
Videos of vortex dynamics in cavity-grade Nb (RRR>300) can be found in Ooi et al., PRB 111, 094519 (2025)
See also,
A. Gurevich and G. Ciovati, PRB 87, 054502 (2013)
A. Romanenko et al., Appl. Phys. Lett. 105, 234103 (2014).
S. Huang eta al., Phys. Rev. Accelerators and Beams 19, 082001 (2016).
S. Posen et al., J. Appl. Phys. 119, 213903 (2016).
S. Ooi et al., Physical Review B 104, 064504 (2021).
S. Ooi et al., Physical Review B 111, 094519 (2025)
Microwave-driven vortex dynamics cause dissipation, which is only weakly dependent on temperature, leading to an elevated surface resistance:
microwave
current
vortex
Vortex
current
Figures adapted from Ooi et al., PRB 111, 094519 (2025)
© American Physical Society.
Dominant cause of in SRF cavities is
Vortices trapped during cool down

## Slide 26
microwave
current
vortex
Vortex
current
Two-level system defects
See also a review:
Müller et al Rep. Prog. Phys. 82, 124501 (2019)
Tunneling
atom
Vortices trapped during cool down
See also,
A. Gurevich and G. Ciovati, PRB 87, 054502 (2013)
A. Romanenko et al., Appl. Phys. Lett. 105, 234103 (2014).
S. Huang eta al., Phys. Rev. Accelerators and Beams 19, 082001 (2016).
S. Posen et al., J. Appl. Phys. 119, 213903 (2016).
S. Ooi et al., Physical Review B 104, 064504 (2021).
S. Ooi et al., Physical Review B 111, 094519 (2025)

## Slide 27
microwave
current
vortex
Vortex
current
Two-level system defects
See also a review:
Müller et al Rep. Prog. Phys. 82, 124501 (2019)
Tunneling
atom
Subgap states
Long MFP
See also, A Gurevich and T Kubo, Physical Review B 96, 184515 (2017)
Vortices trapped during cool down
Short MFP
See also,
A. Gurevich and G. Ciovati, PRB 87, 054502 (2013)
A. Romanenko et al., Appl. Phys. Lett. 105, 234103 (2014).
S. Huang eta al., Phys. Rev. Accelerators and Beams 19, 082001 (2016).
S. Posen et al., J. Appl. Phys. 119, 213903 (2016).
S. Ooi et al., Physical Review B 104, 064504 (2021).
S. Ooi et al., Physical Review B 111, 094519 (2025)
Figures adapted from T. Kubo, Physical Review Applied 17, 014018 (2022)
© American Physical Society.

## Slide 28
microwave
current
vortex
Vortex
current
Two-level system defects
See also a review:
Müller et al Rep. Prog. Phys. 82, 124501 (2019)
Tunneling
atom
Subgap states
Long MFP
Short MFP
See also, A Gurevich and T Kubo, Physical Review B 96, 184515 (2017)
Figures adapted from T. Kubo, Physical Review Applied 17, 014018 (2022)
© American Physical Society.
T. Kubo (2020) not published
Nonequilibrium quasi particles and Nonequilibrium distribution function
t/tau (tau ~ 0.2ns for Nb)
Vortices trapped during cool down

## Slide 29
In such a seemingly complex situation,
how do accelerator researchers extract
high cavity performance?
T Kubo et al., In-house production of a large-grain single-cell cavity at cavity fabrication facility and results of performance tests, IPAC2014, Dresden, Germany, WEPRI022, p.2519
https://doi.org/10.18429/JACoW-IPAC2014-WEPRI022
The accelerator community can build
the best cavities on the planet — achieving .
ILC recipe
← This is not special but typical in accelerator experiments

## Slide 30
Nb cavity technology
for accelerators:
Classical ILC recipe as a representative example
2013 T. Kubo

## Slide 31
270 mm
RRR>300
High purity Nb

## Slide 32
Wire-EDM
(Electrical discharge machining)
Let’s start fabrication.

## Slide 33
Electron beam welding
Half cell + beam pipe
Cavity material quality is maintained
Half cells

## Slide 34
Inside the chamber
Electron gun

## Slide 35
Electron gun
Electron beam

## Slide 36
Electron beam

## Slide 37
Electropolishing (EP)
The electrolyte is a mixture of (9:1) sulfuric acid and hydrofluoric acid (HF).
A DC voltage is applied with Nb as the anode and aluminum as the cathode.
Niobium is oxidized to form Nb2O5.
This oxide layer is dissolved and polished away by HF​ present in the electrolyte.

## Slide 38
Electropolishing (EP)
The electrolyte is a mixture of (9:1) sulfuric acid and hydrofluoric acid (HF).
A DC voltage is applied with Nb as the anode and aluminum as the cathode.
Niobium is oxidized to form Nb2O5.
This oxide layer is dissolved and polished away by HF​ present in the electrolyte.

## Slide 39
B. Aune et al.,
in proceedings of LINAC1990, Albuquerque, New Mexico, USA (1990)
“Q-disease” due to niobium hydride
To degas hydrogen — prevents hydrogen Q-disease (requires >700 ℃)
Annealing

## Slide 40
B. Aune et al.,
in proceedings of LINAC1990, Albuquerque, New Mexico, USA (1990)
“Q-disease” due to niobium hydride
To degas hydrogen — prevents hydrogen Q-disease (requires >700 ℃)
To reduce pinning centers — minimizes trapped flux (requires ~900 ℃)
Annealing
S. Posen et al., J. Appl. Phys. 119, 213903 (2016).
https://doi.org/10.1063/1.4953087

## Slide 41
A second EP step, removing only a few microns.

## Slide 42
Courtesy of Mathieu Omet (KEK)
H. Sakai et al.,
Phys. Rev. Accel. Beams 22,022002 (2019)
https://doi.org/10.1103/PhysRevAccelBeams.22.022002
P. Bernard et al., In proceedings of EPAC1992, Berlin, Germany (1992)

## Slide 43
Courtesy of Mathieu Omet (KEK)
120℃ー48h bake
Without baking
With
baking
Spatial variation of the mean free path on the scale of the penetration depth suppresses the surface current, thereby increasing the maximum achievable field.
L. Lilje et al., in Proceedings of SRF1999, Santa Fe, New Mexico, USA (1999), p. 74, TUA001.
T. Kubo, Supercond. Sci. and Technol. 30, 023001 (2017); Sci. and Technol. 34, 045006 (2021)
V. Ngampruetikorn and J. A. Sauls, Phys. Rev. Research 1, 012015(R) (2019)
High field
Q-drop

## Slide 44
Courtesy of Mathieu Omet (KEK)
120℃ー48h bake
Without baking
With
baking
Spatial variation of the mean free path on the scale of the penetration depth suppresses the surface current, thereby increasing the maximum achievable field.
L. Lilje et al., in Proceedings of SRF1999, Santa Fe, New Mexico, USA (1999), p. 74, TUA001.
T. Kubo, Supercond. Sci. and Technol. 30, 023001 (2017); Sci. and Technol. 34, 045006 (2021)
V. Ngampruetikorn and J. A. Sauls, Phys. Rev. Research 1, 012015(R) (2019)
High field
Q-drop
Labs in Japan and the US traditionally applied a 100℃ bake to remove residual water after high-pressure rinsing. In contrast, labs in Germany and France did not adopt this step — and continued to suffer from the so-called Q-drop.
At the time, the reason was unknown, and the phenomenon was even nicknamed the "European disease.“ It wasn’t until the late 1990s that the community realized the low-temperature bake was the key. This is a prime example of the serendipitous discoveries that have accumulated over the past few decades.

## Slide 46
T Kubo et al., IPAC2014, Dresden, Germany, WEPRI022, p.2519
https://doi.org/10.18429/JACoW-IPAC2014-WEPRI022

## Slide 47
Many modern recipes exist: N-doping, N-infusion, two-step bake, mid-T bakes, etc. They are all variants of the classical recipe, with some steps replaced or modified.
2K
T Kubo et al., In-house production of a large-grain single-cell cavity at cavity fabrication facility and results of performance tests, IPAC2014, Dresden, Germany, WEPRI022, p.2519
https://doi.org/10.18429/JACoW-IPAC2014-WEPRI022
S. Posen et al., Ultralow Surface Resistance via Vacuum Heat Treatment of Superconducting Radio-Frequency Cavities,
Phys. Rev. Applied 13, 014024 (2020)
https://doi.org/10.1103/PhysRevApplied.13.014024
H. Ito et al., Influence of furnace baking on Q–E behavior of superconducting accelerating cavities,
Prog. Theor. Exp. Phys. 2021, 071G01 (2021)
https://doi.org/10.1093/ptep/ptab056
2K
T=2K
ILC recipe
Mid-T bake
Mid-T bake

## Slide 48
2K
T=2K
T Kubo et al., In-house production of a large-grain single-cell cavity at cavity fabrication facility and results of performance tests, IPAC2014, Dresden, Germany, WEPRI022, p.2519
https://doi.org/10.18429/JACoW-IPAC2014-WEPRI022
The accelerator community can build
the best cavities on the planet — achieving .
So why not make use of this technology
in other applications?
ILC recipe
Mid-T bake
Mid-T bake
S. Posen et al., Ultralow Surface Resistance via Vacuum Heat Treatment of Superconducting Radio-Frequency Cavities,
Phys. Rev. Applied 13, 014024 (2020)
https://doi.org/10.1103/PhysRevApplied.13.014024
H. Ito et al., Influence of furnace baking on Q–E behavior of superconducting accelerating cavities,
Prog. Theor. Exp. Phys. 2021, 071G01 (2021)
https://doi.org/10.1093/ptep/ptab056

## Slide 49
Quantum applications
Accelerator cavity
Quantum memory cavity
for quantum computing
Brock et al., Nature 641, 612 (2025)
https://doi.org/10.1038/s41586-025-08899-y

## Slide 50
High-Q superconducting cavities allow us to store quantum information redundantly, enabling bosonic error correction.
1 photon loss
1 photon loss
a remainder of 2
when divided by 3
a remainder of 1
when divided by 3
correct
correct
Known to reduce the required number of qubits by one to two orders of magnitude.
e.g. binomial code
Brock et al., Nature 641, 612 (2025)
https://doi.org/10.1038/s41586-025-08899-y

## Slide 51
Reagor et al., Phys. Rev. B 94, 014506 (2016)
Aluminum,
(single photon level)
3D coaxial cavity progress
Yale University
Brock et al., Nature 641, 612 (2025)
https://doi.org/10.1038/s41586-025-08899-y

## Slide 52
Reagor et al., Phys. Rev. B 94, 014506 (2016)
Aluminum,
(single photon level)
Heidler et al., Phys. Rev. Applied 16, 034024 (2021)
Niobium (1:1:1 buffered chemical polishing at 0-5℃),
(single photon level)
3D coaxial cavity progress
Yale University
Brock et al., Nature 641, 612 (2025)
https://doi.org/10.1038/s41586-025-08899-y
University of Innsbruck

## Slide 53
Reagor et al., Phys. Rev. B 94, 014506 (2016)
Aluminum,
(single photon level)
Heidler et al., Phys. Rev. Applied 16, 034024 (2021)
Niobium (1:1:1 buffered chemical polishing at 0-5℃),
(single photon level)
Oriani et al., Phys. Rev. Applied 24, 044080 (2025)
Niobium (1:1:2 water buffered chemical polishing below 10℃),
(single photon level)
3D coaxial cavity progress
↑
The world record (as of 2024)
Yale University
University of Chicago
Brock et al., Nature 641, 612 (2025)
https://doi.org/10.1038/s41586-025-08899-y
University of Innsbruck

## Slide 54
cavity→
Why don't we give it a shot?
T. Kubo
↓

## Slide 55
T. Kubo
↓
cavity→
Nb coaxial cavity of KEK-NTT collaboration
T. Takenaka, T. Kubo et al.,
arXiv:2510.01819.
Why don't we give it a shot?

## Slide 56
cavity→
Corresponding to
photon lifetime of
~0.1 sec.
T. Takenaka, T. Kubo et al.,
arXiv:2510.01819.
We broke
the world record!!!→
20mK & Single photon level
Nb coaxial cavity of KEK-NTT collaboration
T. Takenaka, T. Kubo et al.,
arXiv:2510.01819.
Why don't we give it a shot?
T. Kubo
↓

## Slide 57
Reagor et al., Phys. Rev. B 94, 014506 (2016)
Aluminum,
(single photon level)
Heidler et al., Phys. Rev. Applied 16, 034024 (2021)
Niobium (1:1:1 buffered chemical polishing at 0-5℃),
(single photon level)
Oriani et al., Phys. Rev. Applied 24, 044080 (2025)
Niobium (1:1:2 water buffered chemical polishing below 10℃),
(single photon level)
T. Takenaka, T. Kubo et al., arXiv:2510.01819 (2025)
Niobium (1:1:1 BCP at 25℃ + 900℃ anneal
+ 1:1:1 BCP flush at 25℃ + 600℃ anneal)
Q=3×109 (single photon level)
3D coaxial cavity progress
Yale University
University of Innsbruck
University of Chicago
T. Takenaka, T. Kubo et al.,
arXiv:2510.01819.
KEK&NTT
The world record
Brock et al., Nature 641, 612 (2025)
https://doi.org/10.1038/s41586-025-08899-y

## Slide 58
Understanding more about physics of Q factor

## Slide 59
T Kubo et al., In-house production of a large-grain single-cell cavity at cavity fabrication facility and results of performance tests, IPAC2014, Dresden, Germany, WEPRI022, p.2519
https://doi.org/10.18429/JACoW-IPAC2014-WEPRI022
Thermally excited
quasiparticles dominate
Dissipation mainly comes from thermally excited quasiparticles at

## Slide 60
T Kubo et al., In-house production of a large-grain single-cell cavity at cavity fabrication facility and results of performance tests, IPAC2014, Dresden, Germany, WEPRI022, p.2519
https://doi.org/10.18429/JACoW-IPAC2014-WEPRI022
Thermally excited
quasiparticles dominate
Dissipation mainly comes from thermally excited quasiparticles at
and
some others at

## Slide 61
T Kubo et al., In-house production of a large-grain single-cell cavity at cavity fabrication facility and results of performance tests, IPAC2014, Dresden, Germany, WEPRI022, p.2519
https://doi.org/10.18429/JACoW-IPAC2014-WEPRI022
A. Romanenko and D. I. Schuster, Understanding Quality Factor Degradation in Superconducting Niobium Cavities at Low Microwave Field Amplitudes, Phys. Rev. Lett. 119, 264801 (2017)
https://doi.org/10.1103/PhysRevLett.119.264801
TLS model explains low-T and low-Eacc nonlinear Q evolution.
Thermally excited
quasiparticles dominate

## Slide 62
T Kubo et al., In-house production of a large-grain single-cell cavity at cavity fabrication facility and results of performance tests, IPAC2014, Dresden, Germany, WEPRI022, p.2519
https://doi.org/10.18429/JACoW-IPAC2014-WEPRI022
TLS model explains low-T and low-Eacc nonlinear Q evolution.
Thermally excited
quasiparticles dominate
T. Takenaka, T. Kubo et al., arXiv:2510.01819.
https://doi.org/10.48550/arXiv.2510.01819
The same is true for the quantum regime
( mK and a tiny photon number)
TLS fit

## Slide 63
T Kubo et al., In-house production of a large-grain single-cell cavity at cavity fabrication facility and results of performance tests, IPAC2014, Dresden, Germany, WEPRI022, p.2519
https://doi.org/10.18429/JACoW-IPAC2014-WEPRI022
Thermally excited
quasiparticles dominate
What about the dissipation mechanisms inherent to superconductors?

## Slide 64
T Kubo et al., In-house production of a large-grain single-cell cavity at cavity fabrication facility and results of performance tests, IPAC2014, Dresden, Germany, WEPRI022, p.2519
https://doi.org/10.18429/JACoW-IPAC2014-WEPRI022
Thermally excited
quasiparticles dominate
M. Martinello et al., Phys. Rev. Lett. 121, 224801 (2018)
DOI: https://doi.org/10.1103/PhysRevLett.121.224801
What about the dissipation mechanisms inherent to superconductors?
1.3GHz

## Slide 65
Mean
free
path
0
Temperature

## Slide 66
Mean
free
path
0
Temperature
Ginzburg-Landau ()

## Slide 67
Mean
free
path
0
Temperature
Ginzburg-Landau ()
Eilenberger
Formalism
Applicable to
Any temperature
Any mean free path

## Slide 68
Mean
free
path
0
Temperature
Ginzburg-Landau ()
Eilenberger
Formalism
Applicable to
Any temperature
Any mean free path
Usadel
Formalism
Applicable to
Any temperature

## Slide 69
Under the ac field
Thermal Equilibrium
Driving force of
Nonequilibrium
Dynamics
(e.g, strength of microwave)

## Slide 70
Linear response
regime
Thermal Equilibrium
Driving force of
Nonequilibrium
Dynamics
(e.g, strength of microwave)
Under the ac field

## Slide 71
Linear response
regime
Thermal Equilibrium
Mattis-Bardeen
Theory
Driving force of
Nonequilibrium
Dynamics
(e.g, strength of microwave)
Under the ac field

## Slide 72
Driving force of
Nonequilibrium
Dynamics
(e.g, strength of microwave)
Linear response
regime
Nonlinear response
Regime
Thermal Equilibrium
Under the ac field
Mattis-Bardeen
Theory

## Slide 73
Driving force of
Nonequilibrium
Dynamics
(e.g, strength of microwave)
Linear response
regime
Nonlinear response
Regime
Thermal Equilibrium
Under the ac field
Mattis-Bardeen
Theory
Unfortunately, this is
the SRF accelerator regime

## Slide 74
Driving force of
Nonequilibrium
Dynamics
(e.g, strength of microwave)
Keldysh
Eilenberger
Linear response
regime
Nonlinear response
Regime
Thermal Equilibrium
Under the ac field
Mattis-Bardeen
Theory
Unfortunately, this is
the SRF accelerator regime

## Slide 75
Driving force of
Nonequilibrium
Dynamics
(e.g, strength of microwave)
Keldysh
Eilenberger
Linear response
regime
Nonlinear response
Regime
Thermal Equilibrium
Under the ac field
Mattis-Bardeen
Theory
Unfortunately, this is
the SRF accelerator regime

## Slide 76
Mattis-Bardeen
Theory
Driving force of
Nonequilibrium
Dynamics
(e.g, strength of microwave)
Keldysh
Eilenberger
Linear response
regime
Nonlinear response
Regime
Thermal Equilibrium
Under the ac field
Unfortunately, this is
the SRF accelerator regime

## Slide 77
Mattis-Bardeen
Theory
Driving force of
Nonequilibrium
Dynamics
(e.g, strength of microwave)
Keldysh
Eilenberger
Linear response
regime
Nonlinear response
Regime
Keldysh-Usadel
Thermal Equilibrium
Under the ac field
Unfortunately, this is
the SRF accelerator regime

## Slide 78
Mattis-Bardeen
Theory
Driving force of
Nonequilibrium
Dynamics
(e.g, strength of microwave)
Keldysh
Eilenberger
Linear response
regime
Nonlinear response
Regime
Keldysh-Usadel
Thermal Equilibrium
Under the ac field
Unfortunately, this is
the SRF accelerator regime

## Slide 79
Mattis-Bardeen
Theory
Keldysh
Eilenberger
Driving force of
Nonequilibrium
Dynamics
(e.g, strength of microwave)
Linear response
regime
Nonlinear response
Regime
Keldysh-Usadel
Thermal Equilibrium
Under the ac field
Unfortunately, this is
the SRF accelerator regime

## Slide 81
Keldysh
Eilenberger
Nonequilibrium
Dynamics
(e.g, strength of microwave)
Linear response
regime
Nonlinear response
Regime
Keldysh-Usadel
Thermal Equilibrium
The SRF accelerator regime

## Slide 82
Keldysh
Eilenberger
Nonequilibrium
Dynamics
(e.g, strength of microwave)
Linear response
regime
Keldysh-Usadel
Thermal Equilibrium
Let us start from
the linear response

## Slide 83
Start from the Keldysh-Eilenberger equations (a set of equations for Green‘s functions and pair potential )
D. Rainer and J. A. Sauls,
Strong coupling theory of superconductivity, in Superconductivity: From Basic Physics to the Latest Developments, edited by P. N. Butcher and Y. Lu (World Scientic, Singapore, 1995), p. 45.

## Slide 84
D. Rainer and J. A. Sauls,
Strong coupling theory of superconductivity, in Superconductivity: From Basic Physics to the Latest Developments, edited by P. N. Butcher and Y. Lu (World Scientic, Singapore, 1995), p. 45.
Start from the Keldysh-Eilenberger equations (a set of equations for Green‘s functions and pair potential )
We apply a small ac electromagnetic field and calculate the first-order perturbation to the current.
Some
factor

## Slide 85
We apply a small ac electromagnetic field and calculate the first-order perturbation to the current.
Then,
the complex conductivity is given by
D. Rainer and J. A. Sauls,
Strong coupling theory of superconductivity, in Superconductivity: From Basic Physics to the Latest Developments, edited by P. N. Butcher and Y. Lu (World Scientic, Singapore, 1995), p. 45.
Start from the Keldysh-Eilenberger equations (a set of equations for Green‘s functions and pair potential )
Some
factor
Some
factor

## Slide 86
W. Zimmermann, E. Brandt, M. Bauer, E. Seider, and L. Genzel, Optical conductivity of BCS superconductors with arbitrary purity, Physica C 183, 99 (1991).
D. Rainer and J. A. Sauls, Strong coupling theory of superconductivity, in Superconductivity: From Basic Physics to the Latest Developments, edited by P. N. Butcher and Y. Lu (World Scientic, Singapore, 1995), p. 45.
T. Kubo, Effects of Nonmagnetic Impurities and Subgap States on the Kinetic Inductance, Complex Conductivity, Quality Factor, and Depairing Current Density, Physical Review Applied 17, 014018 (2022)
Complex conductivity formula for arbitrary MFP (for )

## Slide 87
W. Zimmermann, E. Brandt, M. Bauer, E. Seider, and L. Genzel, Optical conductivity of BCS superconductors with arbitrary purity, Physica C 183, 99 (1991).
D. Rainer and J. A. Sauls, Strong coupling theory of superconductivity, in Superconductivity: From Basic Physics to the Latest Developments, edited by P. N. Butcher and Y. Lu (World Scientic, Singapore, 1995), p. 45.
T. Kubo, Effects of Nonmagnetic Impurities and Subgap States on the Kinetic Inductance, Complex Conductivity, Quality Factor, and Depairing Current Density, Physical Review Applied 17, 014018 (2022)
Complex conductivity formula for arbitrary MFP (for )
In the dirty limit
()
The well-known
dirty-limit Mattis-Bardeen formula

## Slide 88
Keldysh
Eilenberger
Nonequilibrium
Dynamics
(e.g, strength of microwave)
Linear response
regime
Leading order
nonlinear
correction
Keldysh-Usadel
Thermal Equilibrium

## Slide 89
Keldysh–Usadel Equation for SC under a strong ac field
We solve these equations to obtain the nonequilibrium corrections ( and ).
arXiv:2509.09766
To be published in Phys. Rev. Applied https://doi.org/10.1103/8fh8-nknj

## Slide 90
Keldysh–Usadel Equation for SC under a strong ac field
To obtain the current response,
we substitute the solutions (, ) into
We solve these equations to obtain the nonequilibrium corrections ( and ).
← Linear response
← Nonlinear correction of
arXiv:2509.09766
To be published in Phys. Rev. Applied https://doi.org/10.1103/8fh8-nknj

## Slide 91
Schematically, the results can be illustrated as
Linear
response
Nonlinear corrections
← Linear response
← Nonlinear correction of

## Slide 92
Schematically, the results can be illustrated as
Linear
response
Nonlinear corrections
← Linear response
← Nonlinear correction of

## Slide 93
Schematically, the results can be illustrated as
Linear
response
Nonlinear corrections

## Slide 94
Schematically, the results can be illustrated as
Linear
response
Nonlinear corrections
and

## Slide 95
Schematically, the results can be illustrated as
Linear
response
Nonlinear corrections
and
AAA contribution
Contribution mediated
by the nonequilibrium
pair-potential variation

## Slide 96
Schematically, the results can be illustrated as
Linear
response
Nonlinear corrections
and
Time dependent :
Higgs
Time averaged :
Eliashberg effect
Note: This theory automatically includes
the Eliashberg effect (microwave-induced gap enhancement) as well as the Higgs-mode contribution.
AAA contribution
Contribution mediated
by the nonequilibrium
pair-potential variation

## Slide 97
Eliashberg effect?
Higgs?

## Slide 98
Eliashberg effect?
Higgs?
The variation of order parameter does not appear in standard linear-response theories such as Mattis–Bardeen theory because is an effect, but it does emerge in nonlinear response.

## Slide 99
Eliashberg effect?
Higgs?
The variation of order parameter does not appear in standard linear-response theories such as Mattis–Bardeen theory because is an effect, but it does emerge in nonlinear response.

## Slide 100
Eliashberg effect?
Higgs?
The variation of order parameter does not appear in standard linear-response theories such as Mattis–Bardeen theory because is an effect, but it does emerge in nonlinear response.
Time-averaged nonequilibrium gap variation

## Slide 101
Eliashberg effect?
Higgs?
The variation of order parameter does not appear in standard linear-response theories such as Mattis–Bardeen theory because is an effect, but it does emerge in nonlinear response.
Time-averaged nonequilibrium gap variation
Time dependent nonequilibrium gap variation

## Slide 102
Eliashberg effect?
Higgs?
The variation of order parameter does not appear in standard linear-response theories such as Mattis–Bardeen theory because is an effect, but it does emerge in nonlinear response.
Time-averaged nonequilibrium gap variation
Time dependent nonequilibrium gap variation
qausiparticles

## Slide 103
Eliashberg effect?
Higgs?
The variation of order parameter does not appear in standard linear-response theories such as Mattis–Bardeen theory because is an effect, but it does emerge in nonlinear response.
Time-averaged nonequilibrium gap variation
Time dependent nonequilibrium gap variation
Microwave induced
gap enhancement
qausiparticles

## Slide 104
Eliashberg effect?
Higgs?
The variation of order parameter does not appear in standard linear-response theories such as Mattis–Bardeen theory because is an effect, but it does emerge in nonlinear response.
Time-averaged nonequilibrium gap variation
Time dependent nonequilibrium gap variation
Microwave induced
gap enhancement

## Slide 105
Nonlinear correction
arXiv:2509.09766
To be published in Phys. Rev. Applied https://doi.org/10.1103/8fh8-nknj

## Slide 106
Nonlinear correction
arXiv:2509.09766
To be published in Phys. Rev. Applied https://doi.org/10.1103/8fh8-nknj

## Slide 107
Nonlinear correction
Higgs
Contribution:
Time dependent
Eliashberg
Contribution:
Time averaged
arXiv:2509.09766
To be published in Phys. Rev. Applied https://doi.org/10.1103/8fh8-nknj

## Slide 108
Results
arXiv:2509.09766
To be published in Phys. Rev. Applied https://doi.org/10.1103/8fh8-nknj

## Slide 109
Results
The resonance peak at Δ
comes from the Higgs mode
arXiv:2509.09766
To be published in Phys. Rev. Applied https://doi.org/10.1103/8fh8-nknj

## Slide 110
Results
The resonance peak at Δ
comes from the Higgs mode
At lower frequencies,
can be a decreasing function of the ac amplitude (q).
arXiv:2509.09766
To be published in Phys. Rev. Applied https://doi.org/10.1103/8fh8-nknj

## Slide 111
Results
The resonance peak at Δ
comes from the Higgs mode
At lower frequencies,
can be a decreasing function of the ac amplitude (q).
The AAA term is
the dominant contributor
at low frequencies
arXiv:2509.09766
To be published in Phys. Rev. Applied https://doi.org/10.1103/8fh8-nknj

## Slide 112
360MHz for Nb
720MHz for Nb
3.6GHz for Nb
1.8GHz for Nb
ac amplitude dependent dissipative conductivity
Note: this corresponds to a few (mT)
Dirty limit ()
arXiv:2509.09766
To be published in Phys. Rev. Applied https://doi.org/10.1103/8fh8-nknj

## Slide 113
360MHz for Nb
720MHz for Nb
3.6GHz for Nb
1.8GHz for Nb
ac amplitude dependent dissipative conductivity
Note: this corresponds to a few (mT)
Dirty limit ()
Experiments:
Moderately dirty ()
M. Martinello et al., Phys. Rev. Lett. 121, 224801 (2018)
DOI: https://doi.org/10.1103/PhysRevLett.121.224801
M. Martinello et al., PRL. 121, 224801 (2018)
P. Dhakal et al., PRAB 27, 062001 (2024)
arXiv:2509.09766
To be published in Phys. Rev. Applied https://doi.org/10.1103/8fh8-nknj

## Slide 114
360MHz for Nb
720MHz for Nb
3.6GHz for Nb
1.8GHz for Nb
ac amplitude dependent dissipative conductivity
Note: this corresponds to a few (mT)
Dirty limit ()
M. Martinello et al., Phys. Rev. Lett. 121, 224801 (2018)
DOI: https://doi.org/10.1103/PhysRevLett.121.224801
Experiments:
Moderately dirty ()
M. Martinello et al., PRL. 121, 224801 (2018)
P. Dhakal et al., PRAB 27, 062001 (2024)
arXiv:2509.09766
To be published in Phys. Rev. Applied https://doi.org/10.1103/8fh8-nknj

## Slide 115
ac amplitude dependent dissipative conductivity
M. Martinello et al., Phys. Rev. Lett. 121, 224801 (2018)
DOI: https://doi.org/10.1103/PhysRevLett.121.224801
To deal with the red-framed region, the theory must be extended nonperturbatively to capture the quasiparticle spectrum modified by strong AC currents (DOS smearing).
Gurevich, PRL 113, 087001 (2014)
Kubo-Gurevich, PRB 100, 064522 (2019)
Experiments:
Moderately dirty ()
M. Martinello et al., PRL. 121, 224801 (2018)
P. Dhakal et al., PRAB 27, 062001 (2024)

## Slide 116
Keldysh
Eilenberger
Nonequilibrium
Dynamics
(e.g, strength of microwave)
Linear
response
regime
Keldysh-Usadel
Thermal Equilibrium
Leading order
nonlinear
correction
T. Kubo, arXiv:2509.09766
To be published in Phys. Rev. Applied https://doi.org/10.1103/8fh8-nknj

## Slide 117
Keldysh
Eilenberger
Nonequilibrium
Dynamics
(e.g, strength of microwave)
Linear
response
regime
Keldysh-Usadel
Thermal Equilibrium
Leading order
nonlinear
correction
The SRF theory
(Deep Nonlinear Regime)
T. Kubo, arXiv:2509.09766
To be published in Phys. Rev. Applied https://doi.org/10.1103/8fh8-nknj

## Slide 118
Keldysh
Eilenberger
Nonequilibrium
Dynamics
(e.g, strength of microwave)
Linear
response
regime
The SRF theory
(Deep Nonlinear Regime)
Keldysh-Usadel
Thermal Equilibrium
Leading order
nonlinear
correction
Kubo, arXiv:2509.09766
Gurevich, PRL 113, 087001 (2014)
Kubo-Gurevich, PRB 100, 064522 (2019)
T. Kubo, arXiv:2509.09766 (2025)
Nonperturbative treatment (DOS smearing et al.)

## Slide 119
dc + ac

## Slide 120
If the AC field is absent, this reduces to a problem of equilibrium superconductivity.
That case was already well understood decades ago.
See also, T. Kubo, Phys. Rev. Research 2, 033203 (2020); F. Pei-Jen Lin and A. Gurevich, Phys. Rev. B 85, 054513 (2012)
T. Kubo, Phys. Rev. Applied 22, 044042 (2024) DOI: https://doi.org/10.1103/PhysRevApplied.22.044042

## Slide 121
If the AC field is absent, this reduces to a problem of equilibrium superconductivity.
That case was already well understood decades ago.
See also, T. Kubo, Phys. Rev. Research 2, 033203 (2020); F. Pei-Jen Lin and A. Gurevich, Phys. Rev. B 85, 054513 (2012)
T. Kubo, Phys. Rev. Applied 22, 044042 (2024) DOI: https://doi.org/10.1103/PhysRevApplied.22.044042

## Slide 122
If the AC field is absent, this reduces to a problem of equilibrium superconductivity.
That case was already well understood decades ago.
See also, T. Kubo, Phys. Rev. Research 2, 033203 (2020); F. Pei-Jen Lin and A. Gurevich, Phys. Rev. B 85, 054513 (2012)
T. Kubo, Phys. Rev. Applied 22, 044042 (2024) DOI: https://doi.org/10.1103/PhysRevApplied.22.044042

## Slide 123
However, once an AC field is present, the problem becomes much more complicated. In that case, we need to use the theory of nonequilibrium superconductivity.
The Keldysh-Eilenberger theory is a microscopic theory of nonequilibrium superconductivity. It is applicable at any temperature () and for arbitrary mean free path.
The Keldysh–Usadel theory represents the dirty-limit reduction of the Keldysh–Eilenberger theory of nonequilibrium superconductivity, applicable at any T ().
A. Moor et al., Phys. Rev. Lett. 118, 047001 (2017)
T. Jujo, J. Phys. Soc. Jpn. 91, 074711 (2022)
T. Kubo, Phys. Rev. Applied 22, 044042 (2024)
T. Kubo, Phys. Rev. Applied 23, 054091 (2025)

## Slide 124
Keldysh–Usadel Equation: DC Current with AC Perturbation
T. Kubo, Phys. Rev. Applied 23, 054091 (2025)
We solve these equations to obtain the AC-induced nonequilibrium corrections ( and ).
Higgs
↓
T. Kubo, Phys. Rev. Applied 22, 044042 (2024) DOI: https://doi.org/10.1103/PhysRevApplied.22.044042

## Slide 125
Keldysh–Usadel Equation: DC Current with AC Perturbation
To obtain the ac response,
we substitute the solutions (, ) into
We solve these equations to obtain the AC-induced nonequilibrium corrections ( and ).
Higgs
↓
T. Kubo, Phys. Rev. Applied 23, 054091 (2025)
T. Kubo, Phys. Rev. Applied 22, 044042 (2024) DOI: https://doi.org/10.1103/PhysRevApplied.22.044042

## Slide 126
Instead of showing the rigorous algebraic calculations, we will look at schematic illustrations that represent the final results.
T. Kubo, Phys. Rev. Applied 23, 054091 (2025)
T. Kubo, Phys. Rev. Applied 22, 044042 (2024) DOI: https://doi.org/10.1103/PhysRevApplied.22.044042

## Slide 127
Instead of showing the rigorous algebraic calculations, we will look at schematic illustrations that represent the final results.
T. Kubo, Phys. Rev. Applied 23, 054091 (2025)
T. Kubo, Phys. Rev. Applied 22, 044042 (2024) DOI: https://doi.org/10.1103/PhysRevApplied.22.044042

## Slide 128
and
Instead of showing the rigorous algebraic calculations, we will look at schematic illustrations that represent the final results.
T. Kubo, Phys. Rev. Applied 23, 054091 (2025)
T. Kubo, Phys. Rev. Applied 22, 044042 (2024) DOI: https://doi.org/10.1103/PhysRevApplied.22.044042

## Slide 129
and
AAA cotribution
Instead of showing the rigorous algebraic calculations, we will look at schematic illustrations that represent the final results.
T. Kubo, Phys. Rev. Applied 23, 054091 (2025)
T. Kubo, Phys. Rev. Applied 22, 044042 (2024) DOI: https://doi.org/10.1103/PhysRevApplied.22.044042

## Slide 130
and
AAA cotribution
Instead of showing the rigorous algebraic calculations, we will look at schematic illustrations that represent the final results.
Nonequilibrium corrections due to the Doppler fluctuation of flow
T. Kubo, Phys. Rev. Applied 23, 054091 (2025)
T. Kubo, Phys. Rev. Applied 22, 044042 (2024) DOI: https://doi.org/10.1103/PhysRevApplied.22.044042

## Slide 131
Then, the complex conductivity is given by
and
AAA cotribution
Instead of showing the rigorous algebraic calculations, we will look at schematic illustrations that represent the final results.
T. Kubo, Phys. Rev. Applied 23, 054091 (2025)
T. Kubo, Phys. Rev. Applied 22, 044042 (2024) DOI: https://doi.org/10.1103/PhysRevApplied.22.044042

## Slide 132
Complex conductivity formula
case
Nonequilibrium corrections due to the Doppler fluctuation of flow
Higgs
mediated contribution
AAA
contribution
T. Kubo, Phys. Rev. Applied 22, 044042 (2024)
T. Kubo, Phys. Rev. Applied 23, 054091 (2025)

## Slide 133
Complex conductivity formula
case
case
Nonequilibrium corrections due to the Doppler fluctuation of flow
No Doppler fluctuation
Higgs
mediated contribution
AAA
contribution
T. Kubo, Phys. Rev. Applied 22, 044042 (2024)
T. Kubo, Phys. Rev. Applied 23, 054091 (2025)

## Slide 134
ac dc
T. Kubo, Phys. Rev. Applied 22, 044042 (2024)
T. Kubo, Phys. Rev. Applied 23, 054091 (2025)

## Slide 135
ac dc
ac dc
Resonance peak due to the Higgs mode.
Already observed in experiments!
S. Nakamura et al.,
PRL 122, 257001 (2019)
T. Kubo, Phys. Rev. Applied 22, 044042 (2024)
T. Kubo, Phys. Rev. Applied 23, 054091 (2025)
T. Kubo, Phys. Rev. Applied 22, 044042 (2024)
T. Kubo, Phys. Rev. Applied 23, 054091 (2025)

## Slide 136
For , we can analytically calculate the coefficient C
To calculate the kinetic inductance, we just go back to its definition.
Insight for lower frequencies

## Slide 137
For , we can analytically calculate the coefficient C
case
To calculate the kinetic inductance, we just go back to its definition.
Insight for lower frequencies

## Slide 138
case
Higgs
AAA
(23%)
(43%)
For , we can analytically calculate the coefficient C
case
To calculate the kinetic inductance, we just go back to its definition.
Insight for lower frequencies

## Slide 139
case
Higgs
AAA
(23%)
(43%)
For , we can analytically calculate the coefficient C
T. Kubo, Phys. Rev. Applied 22, 044042 (2024)
T. Kubo, Phys. Rev. Applied 23, 054091 (2025)
case
Microscopic theory of
nonequilibrium superconductivity
To calculate the kinetic inductance, we just go back to its definition.
Insight for lower frequencies

## Slide 140
case
Higgs
AAA
(23%)
(43%)
For , we can analytically calculate the coefficient C
T. Kubo, Phys. Rev. Applied 22, 044042 (2024)
T. Kubo, Phys. Rev. Applied 23, 054091 (2025)
case
Semi-phenomenological
Microscopic theory of
nonequilibrium superconductivity
J. R. Clem and V. G. Kogan, Phys. Rev. B 86, 174521 (2012).
T. Kubo, Physical Review Research 2, 033203 (2020).
To calculate the kinetic inductance, we just go back to its definition.
Insight for lower frequencies

## Slide 141
case
Higgs
AAA
(23%)
(43%)
For , we can analytically calculate the coefficient C
T. Kubo, Phys. Rev. Applied 22, 044042 (2024)
T. Kubo, Phys. Rev. Applied 23, 054091 (2025)
case
Fast experiment (Frozen )
Semi-phenomenological
Microscopic theory of
nonequilibrium superconductivity
J. R. Clem and V. G. Kogan, Phys. Rev. B 86, 174521 (2012).
T. Kubo, Physical Review Research 2, 033203 (2020).
To calculate the kinetic inductance, we just go back to its definition.
Insight for lower frequencies

## Slide 142
case
Higgs
AAA
(23%)
(43%)
For , we can analytically calculate the coefficient C
T. Kubo, Phys. Rev. Applied 22, 044042 (2024)
T. Kubo, Phys. Rev. Applied 23, 054091 (2025)
case
Fast experiment (Frozen )
Slow experiment (Oscillating ）
Semi-phenomenological
Microscopic theory of
nonequilibrium superconductivity
J. R. Clem and V. G. Kogan, Phys. Rev. B 86, 174521 (2012).
T. Kubo, Physical Review Research 2, 033203 (2020).
To calculate the kinetic inductance, we just go back to its definition.
Insight for lower frequencies

## Slide 143
“C” from the Keldysh-Eilenberger theory, which is a microscopic theory of nonequilibrium superconductivity and is applicable at any temperature () and for arbitrary mean free path.
Consistent with the dirty limit result
obtained from the Keldysh-Usadel
T. Kubo, Phys. Rev. Applied 22, 044042 (2024)
DOI: https://doi.org/10.1103/PhysRevApplied.22.044042

## Slide 144
We have finally come to understand the true meaning of the semi-phenomenological approach: frozen and oscillating
Frozen
The ac frequency is so fast that
the superfluid density cannot follow it.
(Fast experiment)
What has long been believed
[When Does it happen?]

## Slide 145
Frozen
The ac frequency is so fast that
the superfluid density cannot follow it.
(Fast experiment)
Oscillating
The ac frequency is so slow that the superfluid density can follow it.
(Slow experiment)
[When Does it happen?]
What has long been believed
We have finally come to understand the true meaning of the semi-phenomenological approach: frozen and oscillating

## Slide 146
Frozen
The ac frequency is so fast that
the superfluid density cannot follow it.
(Fast experiment)
Oscillating
The ac frequency is so slow that the superfluid density can follow it.
(Slow experiment)
What has long been believed
We have finally come to understand the true meaning of the semi-phenomenological approach: frozen and oscillating
What has been revealed
by the microscopic theory of nonequilibrum superconductivity
[When Does it happen?]
[When Does it happen?]

## Slide 147
Frozen
The ac frequency is so fast that
the superfluid density cannot follow it.
(Fast experiment)
Oscillating
The ac frequency is so slow that the superfluid density can follow it.
(Slow experiment)
What has long been believed
What has been revealed
by the microscopic theory of nonequilibrum superconductivity
(AAA and Higgs contribution)
wrong
We have finally come to understand the true meaning of the semi-phenomenological approach: frozen and oscillating
[When Does it happen?]
[When Does it happen?]

## Slide 148
The microscopic theory of current dependent
kinetic inductance is established.
case
Higgs
AAA
(23%)
(43%)
case
The Higgs mode is ubiquitous in superconducting devices.
The current dependence of the kinetic inductance is a representative example.
T. Kubo, Phys. Rev. Applied 22, 044042 (2024)
T. Kubo, Phys. Rev. Applied 23, 054091 (2025)

## Slide 149
Condensed matter physics
Astrophysics detectors
Quantum computing
Particle accelerator cavity
Research and development of superconducting resonators, which lie at the intersection of various fields, represent one of the most important efforts to pioneer 21st-century physics.
Summary
T. Kubo (2024)
T. Kubo (2013)
Me
↓
cavity→

## Slide 151
Appendix (1)

## Slide 152
(dirty)
T. Kubo, Phys. Rev. Applied 22, 044042 (2024)
Current dependent
curve
in ac+dc system
dc: arbitrary strength
ac: perturbation

## Slide 153
(dirty)
T. Kubo, Phys. Rev. Applied 22, 044042 (2024)
Let’s see the orange curves (),which correspond to 7GHz for Nb.
7GHz for Nb

## Slide 154
(dirty)
T. Kubo, Phys. Rev. Applied 22, 044042 (2024)
Let’s see the orange curves (),which correspond to 7GHz for Nb.
Dotted curve:

## Slide 155
(dirty)
T. Kubo, Phys. Rev. Applied 22, 044042 (2024)
Let’s see the orange curves (),which correspond to 7GHz for Nb.
Dotted curve:
Dashed curve:
Re[
Significant contribution from
the direct AAA action term

## Slide 156
(dirty)
T. Kubo, Phys. Rev. Applied 22, 044042 (2024)
Let’s see the orange curves (),which correspond to 7GHz for Nb.
Dotted curve:
Dashed curve:
Re[
Solid curve:
Re[
Significant contribution from
the direct AAA action term

## Slide 157
(dirty)
T. Kubo, Phys. Rev. Applied 22, 044042 (2024)
The current-induced reduction of is pronounced as the frequency increases
The key player is the direct AAA photon action
Big clue to understand the pronounced anti Q-slope with increasing frequency
3.6 GHz for Nb
7 GHz for Nb
14 GHz for Nb
36 GHz for Nb
1.8 GHz for Nb

## Slide 158
Appendix (2)

## Slide 159
Purity
(mfp )
Intrinsic
(clean)
any
(from clean limit
to dirty limit)
(e.g., Nb3Sn,
NbN, NbTiN etc.)
(e.g., Nb)
(dirty)
any
(from clean limit
to dirty limit)
N/A
Summary of the superheating field
Theory
(applicable to )
F. Pei-Jen Lin and A. Gurevich,
Phys. Rev. B 85, 054513 (2012)
for
G. Catelani and J. P. Sethna,
Phys. Rev. B 78, 224509 (2008)
F. Pei-Jen Lin and A. Gurevich,
Phys. Rev. B 85, 054513 (2012)
F. Pei-Jen Lin and A. Gurevich,
Phys. Rev. B 85, 054513 (2012)
T. Kubo, Phys. Rev. Research 2, 033203 (2020)
Analytical result for T=0.
V. P. Galaiko, Sov. Phys. JETP 23, 475 (1966)
Analytical result for T=0.
T. Kubo, Phys. Rev. Research 2, 033203 (2020)
T. Kubo, Supercond.Sci. Tecnol. 34, 045006 (2021)
for
for

## Slide 160
Appendix (3)

## Slide 161
T. Kubo, Jpn. J. Appl. Phys. 64, 018002 (2025)
Maximum field achieved so far
Already close to the theoretical limit?
The answer: we currently have no reliable estimate, because there is no theory of applicable to clean Nb at .

## Slide 162
T. Kubo, Jpn. J. Appl. Phys. 64, 018002 (2025)
Maximum field achieved so far
Already close to the theoretical limit?
The answer: we currently have no reliable estimate, because there is no theory of applicable to clean Nb at .
Ginzburg–Landau (GL) theory, valid near , gives
A. J. Dolgert et al., Phys. Rev. B 53, 5650 (1996)
M. K. Transtrum et al., Phys. Rev. B 83, 094505 (2011)

## Slide 163
T. Kubo, Jpn. J. Appl. Phys. 64, 018002 (2025)
Maximum field achieved so far
Already close to the theoretical limit?
The answer: we currently have no reliable estimate, because there is no theory of applicable to clean Nb at .
Ginzburg–Landau (GL) theory, valid near , gives
If we naively extrapolate this to low temperatures — not theoretically justified — we obtain the rough estimate
?
mT ?
A. J. Dolgert et al., Phys. Rev. B 53, 5650 (1996)
M. K. Transtrum et al., Phys. Rev. B 83, 094505 (2011)

## Slide 164
T. Kubo, Jpn. J. Appl. Phys. 64, 018002 (2025)
If we believe this rough
estimate of based on GL, we get
T. Kubo, Jpn. J. Appl. Phys. 64, 018002 (2025)
Note: To achieve , it is necessary to eliminate all surface defects. However, this alone is not sufficient to reach ; it is also essential to ensure that the thermal runaway field exceeds .
This condition is not always satisfied, particularly at 2 K. It is better to test the cavity at lower temperatures (e.g., 1.8K or 1.6K) to ensure that the condition is satisfied.

## Slide 165
Appendix (4)

## Slide 166
The biggest differences between cavities for accelerators and those for quantum applications
photon number
Electric field
distribution
Accelerators
Quantum computing
photon number
K
mK
T. Takenaka, T. Kubo et al.,
arXiv:2510.01819.
T. Kubo et al.,
IPAC2014, Dresden, Germany,
WEPRI022, p.2519